ACCORD CO., LTD.

## 8TH FL., 398, JEN AI ROAD, SEC. 4, TAIPEI, TAIWAN

# TEL:886-2-27044503

##### FAX:886-2-27036358 , 27044593

E-mail: accord@accordia.com.tw

http://www.accordia.com.tw

###### RE: AK-1607-N-BBY-WP-MM

The keypad finish is black baking paint

CONTENTS:

- POLYESTER RESIN

- MELAMINE RESIN

- EPOXY RESIN

- CARBON BLACK

- FILLER

- ORGANIC SOLVENT

- AUXLIARY

The baking paint (coating) can stand the test for salt water spraying over 72 hours.

This keypad can meet the military specification.